Energear EP

Automotive Transmission Oils

_____________________________________________________________________________

Applications

| Designed for use in a wide range of gear units with spur, bevel or helical gear design, including synchronized manual gearboxes, transmissions and axles under moderately severe load and pressure | conditions.It is applicable equally for passenger cars, light and heavy trucks, agricultural and building machinery, even for topping up well run-in hypoid transmission units. |
| --- | --- |

_____________________________________________________________________________

Main Benefits

| *High safety margin against foaming and corrosion. *Reasonable viscosity/temperature and cold flow properties; | *Compatible with all seal and metal types Offers effective protection of gear transmissions prolonging component life |
| --- | --- |

_____________________________________________________________________________

Specifications

| The Energear EP range meet the requirements of API GL-4. The 80W-90 grade also meets ZF TE-ML 02A,16A and 17A. |  |
| --- | --- |

_____________________________________________________________________________

Storage

| All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and | the obliteration of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions. |
| --- | --- |

_____________________________________________________________________________

Health, Safety and Environment

| Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products. | BP p.l.c. or its subsidiaries will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office. |
| --- | --- |

_____________________________________________________________________________

_____________________________________________________________________

Energear EP

Automotive Transmission Oils

_____________________________________________________________________________

Typical Characteristics

_____________________________________________________________________________

|  | Test Methods | Units | Grade : |
| --- | --- | --- | --- |

|  |  |  | 80W-90 | 85W-140 |
| --- | --- | --- | --- | --- |
| Density at 15 °C | ASTM D1298 | kg/cbm | 895 | 908 |
| Kinematic viscosity at 40 °C | ASTM D445 | mm2/s | 137.8 | 414.2 |
| Kinematic viscosity at 100°C | ASTM D445 | mm2/s | 13.9 | 29.3 |
| Viscosity Index | ASTMD2270 |  | 97 | 95 |
| Pour Point | ASTM D97 | °C | -30 | -18 |
| Flash Point (COC) | ASTM D92 | °C | 210 | 220 |

_____________________________________________________________________________

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |

_____________________________________________________________________________