_____________________________________________________________________

____________________________________________________________________________

BP Energol RC-RTM

Air compressor lubricant

____________________________________________________________________________

Description

The Energol RC-R compressor oil range of lubricants are based upon highly refined mineral oils and carefully chosen additives. They are intended for the lubrication of rotary and reciprocating compressors.

_____________________________________________________________________________

Applications

The Energol RC-R grades are ashless oils recommended for the lubrication of rotors, bearings and gears in rotary compressors, especially the oil flooded screw type with delivery temperatures of up to 120°C. Energol RC-R compressor oils exhibit low carbon forming tendencies and meet the requirements of the DIN 51506 VD-L classification for reciprocating compressors having air discharge temperatures up to 220°C. Energol RC-R 32 and 46 are suitable for oil flooded rotary compressors, whilst Energol RC-R 68 and 100 would be selected for lubricating the crankcase and cylinders of reciprocating compressors. Selection of the required viscosity grade should be based upon the compressor manufacturers’ recommendation. The Energol RC-R range is fully compatible with nitrile, silicone and fluropolymer seal materials. Energol RC-R is classified as follows: DIN 51506 VD-L ISO 6743-3 Compressor Oils: DAA and DAB for reciprocating air compressors DAG for rotary air compressors Energol RC-R grades meet the requirements of: Atlas Copco (2000 hour oil) Compair

_____________________________________________________________________________

Advantages

Excellent water separation characteristics allows condensation to readily separate from the oil, minimising the risk of emulsions which could block the oil separator element. Prevents corrosion when operating under humid conditions. Excellent coalescing properties means little carry over of oil in the air stream. Low deposit forming tendencies extends oil change intervals and provides longer air filter life which contributes to a reduction in maintenance costs. Good thermal stability, low volatility and low carbon formation reduces the risk of fire and explosion.

____________________________________________________________________________

Typical Characteristics

| Test | Method | Unit | 32 | 46 | 68 | 100 | 150 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Density @ 15°C | ISO 12185 / ASTM D4052 | g/ml | 0.87 | 0.87 | 0.88 | 0.89 | 0.89 |
| K.V @ 40°C | ISO 3104 / ASTM D445 | mm2/s | 32 | 46 | 68 | 100 | 150 |
| K.V @ 100°C | ISO 3104 / ASTM D445 | mm2/s | 5.57 | 6.67 | 8.57 | 11.4 | 14.5 |
| Viscosity Index | ISO 2909 / ASTM 2270 | - | 110 | 100 | 100 | 98 | 98 |
| Foam Sequence I | ISO 6247 / ASTM D892 | mls/mls | 30/0 | 30/0 | 30/0 | 30/0 | 30/0 |
| Pour Point | ISO 3016 / ASTM D97 | °C | -21 | -21 | -21 | -12 | -9 |
| Flash Point, PMC | ISO 2719 / ASTM D93 | °C | 216 | 222 | 222 | 243 | 246 |
| Rust Test (24 hr synthetic sea water) | ISO / 7210 / ASTM D665B | - | Pass | Pass | Pass | Pass | Pass |
| Conradson carbon residue after aging | DIN 51352/2 | % | 0.7 | 0.7 | 0.7 | <3.0 | <3.0 |
| RPVOT | ASTM D2272 | mins | 270 | 270 | 270 | - | - |

_____________________________________________________________________________

Additional Information

_____________________________________________________________________________

Storage

All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and the obliteration of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions.

_____________________________________________________________________________

Health & Safety Recommendations

Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products.

BP International will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office.

______________________________________________________________________________

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |

_______________________________________________________________________________

BP Energol RC-R is the trademark of bp plc

_______________________________________________________________________________