_______________________________________________________________________

Trafo Yagi
Transformer Oil

__________________________________________________________________________

Description

| BP Trafo Yagi is an inhibited transformer oil meeting the international specifications |  | IEC 296 (82) - Class IA and IIA, ASTM D3487 type II and TEAS. |
| --- | --- | --- |

__________________________________________________________________________

Applications

| For use as a transformer, switchgear and circuit breaker oil which conforms to the international |  | specifiaction IEC 296 (82) - Class IA and IIA, ASTM D3487 type II and TEAS. |
| --- | --- | --- |

__________________________________________________________________________

Main Benefits

| * High dielectric strength and low power-loss, * High oxidation resistance, * Low sludge formation, |  | * Excellent cooling properties, * High purity and high flashpoint. |
| --- | --- | --- |

__________________________________________________________________________

Storage

| All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and the obliteration |  | of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions. |
| --- | --- | --- |

__________________________________________________________________________

Health, Safety and Environment

| Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products. |  | BP p.l.c. or its subsidiaries will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office. |
| --- | --- | --- |

__________________________________________________________________________

Typical Characteristics 
__________________________________________________________________________

|  | Test Methods | Units | Grade : |
| --- | --- | --- | --- |

__________________________________________________________________________

|  |  |  | Trafo Yagi |
| --- | --- | --- | --- |
| Appearance | Visual |  | Clear, Free from Sediment |
| Density | ISO 12185 | kg/m³ | 886 |
| Pour Point | ISO 3016 | °C | -57 |
| Flash Point | ASTM D93 | °C | 148 |
| Kinematic Viscosity | ISO 3104/ASTM D445 | mm²/s |  |
| 40°C |  |  | 8.9 |
| -30°C |  |  | 1180 |
| Neutralisation Value | IEC 296 | mgKOH/g | <0.01 |
| Corrosive Sulphur | ISO 5662 |  | Nil |
| Anti Oxidant Additive |  |  | No |
| Breakdown Volt. (new dry oil) | IEC 156 | KV | 40-60 |
| Dissipation F.at 90°C, 50 Hz | IEC 247 |  | <0.001 |
| Oxidation Stability: | IEC1125B |  |  |
| Induction period |  | h | >170 |
| Sludge Free Life |  | h | >88 |

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. |  | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |  |