Vanellus Super V Turbo 15W-40

High performance diesel engine oil

_____________________________________________________________________________

Applications

| Vanellus Super V Turbo is a four-seasons engine oil specifically designed for the new generation turbo and supercharged diesel engines providing high protection, resistance to wear and excellent engine cleanliness by its new Thermo Active formula | The special Thermo Active formula of Vanellus Super V Turbo results in excellent protection and consistent performance even at the highest working temperatures. This formula provides a shield which protects the engine even better as the temperature rises. It is proved that it provides up to 50% higher protection than its equivalents at all weather conditions, heavy duty and road types. |
| --- | --- |

_____________________________________________________________________________

Main Benefits

| Decreases maintenance costs in turbo and supercharged diesel engines by protecting against wear by the Thermo Active formula. | Provides excellent engine cleanliness resulting longer engine life. Provides longer drain intervals as the oil does not diminish and the oil pressure does not decrease. |
| --- | --- |

_____________________________________________________________________________

Specifications

| Vanellus Super V Turbo 15W-40 meets the following specifications: • API CG-4/SG | Suitable for use in MB and MAN engines. |
| --- | --- |

_____________________________________________________________________________

Storage

| All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and | the obliteration of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions. |
| --- | --- |

_____________________________________________________________________________

Health, Safety and Environment

| Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products. | BP p.l.c. or its subsidiaries will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office. |
| --- | --- |

_____________________________________________________________________________

_____________________________________________________________________

Vanellus Super V Turbo 15W-40

High performance diesel engine oil

_____________________________________________________________________________

Typical Characteristics

_____________________________________________________________________________

|  | Test Methods | Units | Grade : |
| --- | --- | --- | --- |

_____________________________________________________________________________

_____________________________________________________________________________

|  |  |  | SAE 15W-40 |
| --- | --- | --- | --- |
| Density at 15 °C | ISO3675/ASTM D1298 | kg/m³ | 887 |
| Kinematic Viscosity at 100 °C | ISO3104/ASTM D445 | mm²/s | 14.7 |
| at 40 °C | ISO3104/ASTM D445 | mm²/s | 113.5 |
| Viscosity Index | ISO2909/ASTM D2270 | - | 134 |
| CCS Viscosity at -20 °C | ASTM D2602 | mPa.s | 6800 |
| Pour Point | ISO3016/ASTM D97 | °C | -31 |
| Flash Point (COC) | ISO2592/ASTM D92 | °C | 222 |
| Total Base Number | ISO 3771/ASTM D2896 | mgKOH/g | 11.7 |

_____________________________________________________________________________

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |

_____________________________________________________________________________