_________________________________________________________________

Visco 7000 0W-40

_________________________________________________________________
Applications

| Visco 7000 0W-40 is a fully synthetic engine oil suitable for use in modern gasoline and diesel automotive engines including turbo-charged, intercooled and direct injection diesel. Including diesel vehicles fitted with particulate filters. |  |  |
| --- | --- | --- |

_________________________________________________________________

Main Benefits

| Ultimate cleaning performance over extended service intervals Exceptional protection for modern engines Excellent emissions reduction Optimized cold start High fuel efficiency |  |  |
| --- | --- | --- |

_________________________________________________________________

Specifications

| API SM/CF ACEA A3/B3, A3/B4, C2, C3 |  | BMW Longlife-04 (do not use in gasoline engines outside the EU) VW 502 00/ 503 01/ 505 00 MB-Approval 229.31/229.51 All Porsche vehicles except Cayenne V6 |
| --- | --- | --- |

_________________________________________________________________

Storage

| All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and |  | the obliteration of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions. |
| --- | --- | --- |

_________________________________________________________________

Health, Safety and Environment

| Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products. |  | BP p.l.c. or its subsidiaries will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office. |
| --- | --- | --- |

_________________________________________________________________

Typical Characteristics 
_________________________________________________________________

|  | Test Methods | Units | Grade : |
| --- | --- | --- | --- |

_________________________________________________________________

|  |  | SAE 0W-40 |
| --- | --- | --- |

_________________________________________________________________

| Test | Method(s) | Unit | Typical |
| --- | --- | --- | --- |
| Density @ 15C, Relative | ASTM D4052 | g/ml | 0.838 |
| Viscosity, Kinematic 100C | ASTM D445 | mm²/s | 12.8 |
| Viscosity, Kinematic 40C | ASTM D445 | mm²/s | 75.7 |
| Viscosity, CCS -35C (0W) | ASTM D5293 | cP | 5850 |
| Flash Point, PMCC | ASTM D93 | °C | 244 |
| Ash, Sulphated | ASTM D874 | % wt | 0.7 |
| Total Base Number, TBN | ASTM D2896 | mg KOH/g | 6.4 |

_________________________________________________________________

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. |  | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |  |